|  | STUFFING BOX PACKINGS |
| --- | --- |
|  | AVKOPACK 1101/101 |  |
|  | documentation |  |
|  | Composition | PTFE + lubricant |

|  | AVKOPACK 1101S/101S |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | PTFE |

|  | AVKOPACK 1120/120 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | PTFE/graphite + lubricant |

|  | AVKOPACK 1120G |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | PTFE/graphite + lubricant |

|  | AVKOPACK 1201/201 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | aramid, PTFE + lubricant |

|  | AVKOPACK 1201P/201P |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | staple aramid, PTFE + lubricant |

|  | AVKOPACK 1201M |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | m-aramid, PTFE + lubricant |

|  | AVKOPACK 1202/202 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | PTFE/graphite/ aramid + lubricant |

|  | AVKOPACK 1203/203 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | PTFE/aramid + lubricant |

|  | AVKOPACK 1301/301 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | carbon fibres + lubricant |

|  | AVKOPACK 1302/302 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | carbonised fibres + PTFE |

|  | AVKOPACK 1320*/320* |  |
| --- | --- | --- |
|  | documentation |  |
|  | Series stuffing box packing braided from expanded graphite yarn. Depending on the type of the yarn are offered different kinds of packings according to the requirement to exploitation characteristics. |
|  | Carring fibre | Type packing |
|  | cotton | AVKOPACK ® 1320 C |
|  | glass | AVKOPACK ® 1320 G |
|  | aramid | AVKOPACK ® 1320 K |
|  | carbon | AVKOPACK ® 1320 B |
|  | cotton+inconel | AVKOPACK ® 1320 CI |
|  | glass+inconel | AVKOPACK ® 1320 GI |
|  | inconel | AVKOPACK ® 1320 I |
|  | polyamid | AVKOPACK ® 1320 P |
|  | cotton+steel | AVKOPACK ® 1320 CS |
|  | glass+steel | AVKOPACK ® 1320 GS |
|  | stainless steel | AVKOPACK ® 1320 S |
|  | outer cabling with inconnel | AVKOPACK ® 1320 X |

|  | AVKOPACK 1320X |  |
| --- | --- | --- |
|  | documentation |  |
|  |  | AVKOPACK 1320X is a diagonally braided packing, manufactured after a special technology in order to guarantee high exploitation parameters. |

|  | AVKOPACK 1331 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | exp. graphite / carbon |

|  | AVKOPACK 1360 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | exp. graphite / ceramic |

|  | AVKOPACK 1400/400 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | cotton, PTFE + lubricant |

|  | AVKOPACK 1401/401 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | ramie, PTFE + lubricant |

|  | AVKOPACK 1402/402 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | cotton + lubricant |

|  | AVKOPACK 1402G/402G |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | cotton, graphite + lubricant |

|  | AVKOPACK 1502/502 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | glass |

|  | AVKOPACK 1502H |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | glass + special silicate system |

|  | AVKOPACK 1513 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | glass, PTFE, graphite |

|  | AVKOPACK 1520 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | glass, PTFE |

|  | AVKOPACK 1530 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | glass, graphite |

|  | AVKOPACK 1602/602 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | ceramic |

|  | AVKOPACK 1720/720 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | Acrylic, PTFE |

|  | AVKOPACK 1730 |  |
| --- | --- | --- |
|  | documentation |  |
|  | Composition | Novoloid, PTFE + lubricant |

|  | AVKOTOOL 11 - DEVICE FOR CUTTING OF PACKINGS |
| --- | --- |
|  | Used for cutting of stuffing box packing at length determined by the diameter of the shaft and the dimensions of the vertical section of the packing. Gives a possibility of working at a maximum diameter of the shaft up to 140 mm. The maximum size of the packing is 25 x 25 mm. The usage of this instrument garantees the cutting of the packing at the length and reqiured angle needed for achieving a maximum jointing effect. A precisely cut packing decreases the appearance of relatively soft areas, the waste of material and time. |

|  | AVKOTOOL 12 - EXTRACTORS |
| --- | --- |
|  | The extractors take apart the used stuffing box packings from the deep hardly reachable parts of the stuffing boxes. The presence of even minimal quantity of the old dry and compressed stuffing box packings may decrease to minimum the effect of its change with a new one, because this leads to increased wearing out of the shaft and unwanted leaking of the working fluid. |

|  |  | PACKING PRODUCING MACHINES |
| --- | --- | --- |
|  | Description of the machines The high-qualified AVKO knitting machines are elaborated and produced as a result of many years’ works in the area of the industrial insulation materials. The direct supervision of their performance in the production process gives the opportunity for a permanent improvement of the producing machines, for the complete satisfaction of the highly set requirements of the contemporary insulation materials. The diagonally AVKO knitting machines are used for the production of high-quality stuffing box packing, cords, ropes. The construction of the machines gives the opportunity for the product to be impregnated if necessary, at regulated temperature of the impregnator. The machines are easily knitting two-, three- and four-diagonal insulating products as well as from high-qualified yarns as aramide, PTFE, carbon fiber, glass fiber, ceramic. etc. The supply with universal brackets allows the simultaneous usage of several types of yarns. Due to the glass-aluminum defense the machines with lowered level of noise allows a permanent control on the technological process. The high reliability of the machines allows their exploitation at three-shift rate. Advantages Minimum dust in the working area due to the presence of a plug-in inlet for the aspiration system; Unleveled easy electronic regulation of the speed of the machine, depending on the yarns used; Regulation of the yarn tension for obtaining various densities of the packing; Electronic regulation of the temperature of the impregnation bath and its visualization; Electronic counter of the length of the produces packing, in meters; Electronic counter of the wrking hours of the machines; Fast change of the calibrating element; Easy service; High productivity; Technical characteristics Parameter Measure unit Model of the machine AV 8 2 x AV 12 AV24 Head numbers pcs. 1 2 1 Bracket number pcs. 8 2 x 12 24 Dimensions range mm 3x3÷6x6 6x6÷12x12 8x8÷22x22 Diagonal numbers pcs. 2 3 4 Delivery voltage V 380 V - 50 Hz 380 V - 50 Hz 380 V - 50 Hz Capacity of the el. motor kW 0,55 2 x 0,75 1,5 Revolutions of the el. motor min-1 750 750 1000 Dimension of the coils Ø x L mm 70 / 250 70 / 250 70 / 250 Outside dimensions L x B x H mm 1210 / 900 / 1720 1670 / 1210 / 1720 1560 / 1550 / 2600 Weight kg 700 1200 1500 |

| PACKING INSTALLATION PROCEDURES |
| --- |
|  | In order to be increased the term of exploitation of the machines and the equipment and also in order to be secured their reliability it is necessary for you to follow the Instruction for installation of packings. It is recommended from ESA (European Sealing Association). We are members of ESA. Instruction is available in PDF format. |
|  | download |

|  | Pre-insulated Piping Systems (PIPS) |
| --- | --- |
|  | The Pre-insulated Piping Systems (PIPS) supplied by AVKO jsc have the following major advantages: Excellent heat insulating characteristics, resulting in minimal heat losses. Exceptional durability - the PUR insulation layer is characterized with exploitation term up to 30 years at working temperature of the heat carrier of 120 °C. In case the temperature of the working fluid is lower the exploitation term is longer. Easy, fast and economically advisable installing process, compared to the traditional building of district heat pipelines - for each particular project it is possible to be designed specific fittings and joints. It is possible to be built in electronic system to indicate and locate any leeks along the pipeline as well as any oozing of moisture in the insulation layer. Our production program include both most common monitoring systems - Brandes and Nordic wire. |
|  | Materials used for the production of pre-insulates piping systems |
|  | All of the materials as well as their quality conform to BSS EN 253:2003 and BSS EN 448:2003. Carrier pipe Steel welded pipes that conforming to EN 10217, DIN 1626 Steel seamless pipes that conform to EN 10216, DIN 1629 Heat insulating layer of PUR foam This foam is a two-component system (mixture of polyol and isocianate) with foaming agent pentane, CO2 or another (we do not use freon systems). The ready mixture has homogeneous cellular structure with average heat conductivity factor less than 0,034 w/mK. Jacket HDPE pipe (high-density polyethylene) |

|  | Pre-insulated pipes |
| --- | --- |
|  | Technical data: |

|  | Pre-insulated elbows |
| --- | --- |
|  | Pre-insulated elbow 90° |
|  | Technical data: |
|  | Pre-insulated elbow 45° |
|  | Technical data: |
|  | Pre-insulated t-branch |
|  | Pre-insulated straight t-branch |
|  | Technical data: |
|  | Pre-insulated edge t-branch |
|  | Technical data: |
|  | Pre-insulated parallel t-branch |
|  | Technical data: |

|  | Anchor |
| --- | --- |
|  | Technical data: |

|  | Pre-insulated reductions |
| --- | --- |
|  | Technical data: |

|  | Compensators |
| --- | --- |
|  | Technical data: |

|  | Pre-insulated valves |
| --- | --- |
|  | Pre-insulated closing valve |
|  | Technical data: |
|  | Pre-insulated drainage valve |
|  | Technical data: |

|  | Thermoshrincable muffs |
| --- | --- |
|  | Technical data: |

|  | Accessories |
| --- | --- |
|  | AVKO jsc also supplies completing products for building of pre-insulated piping systems, including: end caps end shrinkable sleeves seal rings foam pads |

|  | Cold bent steel elbows |
| --- | --- |
|  | The cold bent elbows are produced from longitudinally welded steel pipes, which conform to EN 10217-2 or DIN 1626. The bent elbow satisfies the quality requirements, stated in EN 448:2003. Standard sizes include DN 20 to DN 200 with angle 45° and 90° and bending radius 2,5D. On request it is possible to be manufactured elbows with different angle and length of the legs. |
|  | Technical data |

|  | Forged steel fittings with welded legs |
| --- | --- |
|  | Forged steel elbows |
|  | These elbows consist of a forged fitting conforming to ASME/ANSI B 16.9 / B 16.28 or DIN 2605-1991 with bending radius 1,5D to which there are welded longitudinally welded steel pipes conforming to EN 10217 or DIN 1626. The quality of the welding seams conforms to BSS EN 25817-B. Standard offered sizes include DN 20 to DN 400 with angle 45° and 90°. On request it is possible to be manufactured elbows with different sizes. |
|  | Technical data |
|  | Forged steel reductions |
|  | These reductions consist of a forged fitting conforming to ASME/ANSI B 16.9 or DIN to which there are welded longitudinally welded steel pipes conforming to EN 10217 or DIN 1626. The quality of the welding seams conforms to BSS EN 25817-B. Standard offered sizes include DN 25/20 to DN 250/200. On request it is possible to be manufactured reductions with different sizes . |
|  | Technical data |
|  | Forged steel tee-pieces |
|  | Forged tee-pieces are manufactured in three types – straight, angular and parallel. Each type can be produced by using either forged tee piece with equal sizes in all ends, or reduction tee piece. The quality of the welding seams conforms to BSS EN 25817-B. Standard offered sizes include DN 20 to DN 400. On request it is possible to be manufactured tee-pieces with different sizes. |
|  | Technical data |

|  | Properties of polytetrafluorethylene (PTFE) made products |
| --- | --- |
|  | The chemical structure of PTFE is a long carbon chain surrounded by fluoride atoms in a kind of protective casing. This chemical structure predetermines the exceptional properties and numerous applications of PTFE, making it completely different from the rest of polymers. |
|  | PTFE products guarantee: |
|  | Reliable service at temperatures above the temperature range of all thermoplastic materials. In various working media, service temperature can reach up to 260 °Ѡfor continuous service. PTFE remains stable even when exposed to temperatures of -200 °ѻ Excellent anti-aging property even at higher temperatures and in the presence of solvents, oils, oxidizers, UV radiation, or other kind of working environment's impact; PTFE is biologically resistant to ferments and microbes. It is chemically pure and inert, therefore does not affect the working environment; Extremely non-adhesive as a solid material, PTFE has very low surface tension - viscose, volatile or squashy liquids do not stick to the contacting surfaces. Allows excellent washing and sterilizing; Impervious to the most corrosive organic and inorganic chemical compounds; High electrical resistance; Nonflammable; Low thermal conductivity; Lowest coeficient of friction compared to any other similar material; Wear property can be made appropriate for any working environment by adding high-purity fillers, such as graphite, molybdenum disulfide, glass, or bronze. |

|  | SEMI-FINISHED PRODUCTS AVKOFLON® |
| --- | --- |
|  | :: MATERIALS |
|  | - pure PTFE; - PTFE with glass filler; - PTFE with graphite filler; - PTFE with coal filler; - PTFE with molybdenum disulfide filler; - PTFE with bronze filler. |
|  | :: SHEETS |
|  | Standard sizes *, mm 300x300;500x500;600x600;1000x1000;1200x1200 Standard thicknesses *, mm 1, 2, 3, 4, 5 . . . 100 |
|  | :: PRESSED RODS |
|  | Standard sizes*, mm 32 38 45 55 60 70 80 90 100 110 120 135 145 160 175 195 35 40 50 58 65 75 85 95 105 115 125 140 150 165 185 200 |
|  | Allowable size tolerance*, mm Diameter up to 40 40÷70 70÷80 80÷100 over 100 Tolerance +2 +2.8 +3.2 +4.0 on request |
|  | Standard heights , mm max 230 Allowable height tolerance*, mm ±10 |
|  | :: PRESSED TUBES |
|  | Standard sizes* (D x d, mm) 32x20 60x25 70x50 80x40 90x55 110x75 145x85 195x170 35x25 60x30 70x55 80x45 94x45 115x80 145x100 225x50 38x18 60x35 75x20 80x50 94x55 115x90 145x120 225x190 42x18 60x40 75x25 80x55 94x60 120x40 150x100 235x195 45x25 65x20 75x30 80x60 94x65 120x65 150x105 235x205 50x20 65x25 75x35 85x30 100x30 120x75 160x125 305x285 50x25 65x30 75x40 85x40 100x45 120x100 160x130 380x340 50x30 65x35 75x45 85x50 100x55 120x105 165x140 430x383 50x35 65x45 75x50 85x55 100x60 125x80 174x122 630x577 55x25 65x50 75x55 85x60 100x70 135x75 174x140 55x30 70x20 75x60 85x65 100x75 135x85 185x155 55x35 70x25 80x20 90x25 100x80 135x105 185x160 55x40 70x30 80x25 90x40 100x85 140x75 185x165 55x45 70x40 80x30 90x45 100x90 140x95 195x155 60x20 70x45 80x35 90x50 105x65 140x110 195x165 |
|  | Allowable size tolerance*, mm Diameter up to 50 50÷70 70÷90 90÷110 110÷150 over 150 Tolerance D d +2.0 -2.0 +2.8 -2.8 +3.6 -3.6 +4.9 -4.0 +7 -6 +max 20 -max 20 |
|  | Standard heights, mm max 230 Allowable height tolerance*, mm ±10 |
|  | * Other sizes and tolerances - on request |

|  | READY-MADE PRODUCTS AVKOFLON |
| --- | --- |
|  | PTFE extruded rods Standard sizes*, (D, mm) ø6 ÷ ø205 Standard lengths, (m) 1; 2 Tolerances* Diameter: <10 10 ÷ 20 20 ÷ 30 30 ÷ 50 50 ÷ 100 >100 D +0.4 +0.5 +1.0 +1.5 +2.0 +4.0 PTFE extruded tubes Standard sizes*, (D, mm) 10x5 ÷360x150 Standard lengths, (m) 1; 2 Tolerances* Diameter: <10 10 ÷ 20 20 ÷ 30 30 ÷ 50 50 ÷ 100 >100 D +0.5/-0.5 +0.5/-0.5 +1.0/-1.0 +1.5/-1.5 +2.0/-2.0 +4.0/-3.0 Flat gaskets Description: Flat gaskets made of pure or filler-loaded PTFE. Intended use: For sealing of the flanges of pipes, valves, fittings, containers etc. made of steel, glass, plastics, or ceramics. Envelope gaskets Description: Flat gaskets made of pure PTFE with insertion. Application: For sealing of flanges, valves, tanks, boilers, mixers, etc. products, made of steel, glass, plastics, ceramics, or graphite. Sealing on the inside diameter Sealing on the outside diameter PTFE sliding bearingd Application: Applied in machine joints to secure the support and relative translation of individual machine parts. Used also in bridge engineering, construction of chimneys, buildings, tunnels, pipelines, etc. Advantages of PTFE, determining its wide application range: - Extremely low coefficient of friction; - Chemically inert; - Excellent chemical resistance; - High service temperature, stability from -200°C up to +260°C; - Low nad steady wear factor; - Excellent dielectric properties, thermal insulator; - Abrasion-resistant; - Anti-aging and non-fatigue properties; - No need for lubrication. Most commonly used materials: PTFE with glass filler, PTFE with MoS2 filler, PTFE with bronze filler, PTFE with graphite filler. "O" - Rings Application: The use of "O"-rings is based on an initial small deformation at the time of fitting, which secures reliable sealing properties during contact with the sealed-in fluid. O-rings can be placed on static machine parts, as well as on rotating, or reciprocating parts. Advantages: Exhibits excellent resistance to extreme high temperatures in a chemically aggressive environment. Standard sizes * D >12 >20 >25 >30 >80 >200 d 3 ±0.1 4 ±0.1 5 ±0.1 6 ±0.2 7 ±0.2 8 ±0.3 9 ±0.4 10 ±0.41 Standard types Glass-PTFE cloth Description: A material that combines the properties of glass cloth with the specific properties of PTFE coating and is applied in chemical and food industry, electrical engineering, packaging industry, construction, etc. Service temperature range between -200°C and +260°C. Standard sizes: Rolls Width (mm): 1000; Thickess (mm): 0.10, 0.13, 0.15, 0.25; Lengths (m): 30, 50, 100; Variants: with or without self-adhesive layer; Antistatic excution on request. Rolls Width (mm): 35; Thickess (mm): 0.13; Lengths (m): 50; Self-adhesive 5 mm strip along the edges. Piston rings and stuffing-box elements made from filled PTFE Application: The set of rider and sealing rings provides reliable sealing between the piston and the cylinder bush, and the set of single-, double- and triple stuffing-box elements provides the sealing of the piston rod. Advantages: Piston rings and stuffing-box elements made of PTFE filled with graphite, coal, coke, bronze or other fillers, display a series of specific properties: low friction coefficient, extremely high wear resistance and extended service life, no need for lubrication, simplified junction structure, and ensured purity of technological processing wherever necessary. Sizes: Manufactured after customer-provided drawings, no limitations as to sizes or shape. |

|  | LINING WITH PTFE AND FLUOROPLASTICS |
| --- | --- |
|  | PTFE-lined heating bodies |
|  | Application: For heating and temperature maintenance in aggressive fluids with ph 0-14, applied in electrodeposition, etc. |
|  | Structure: A metal heating pipe with protective grounding, PTFE-lined, hence, provided with the following advantages: - extended service life and applicability for all electrolytes; - smooth non-sticky surface determined by the anti-adhesive properties of material; - easy cleaning PTFE-made restrictors preventing the heating body from touching the tub wall. Marked minimal depth of dipping, preventing the heater from overloads. Airtight connecting box. |
|  | PTFE lined hoses |
|  | PTFE-lined corrugated and smooth-surface hoses are based on PTFE flexible tube with metal or rubber armour. They combine a number of properties: Exceptional chemical resistance, resulting from the PTFE flexible tube, which is placed in direct contact with the transferred fluid, thus making the product corrosion-proof; Wide service temperature range from -70°C up to +230°C, depending on the working pressure; Excellent flexibility as a result from the appropriately corrugated PTFE flexible tube; High working pressure resistance, vacuum and hydraulic impact resistance coming as a result from the built-in flexible tube reinforced with steel spiral, and the outside metal stainless steel braiding or rubber flexible tube; The passing fluids is 100% transferred due to the anti-adhesive properties of PTFE, and excellent self-cleaning is also effected. |
|  | Tanks, pipes, fittings and fixtures with industrial PTFE and fluoroplastic lining |
|  | Applications: For preserving and transporting chemically aggressive fluids, concentrated acids, bases, petrol products, etc. PTFE is known for its universal chemical resistance, which enables its wide application in the production of storage vessels and transportation pipelines for various chemicals. Steel or reinforced plastic tanks can be used for highly corrosive materials, when lined with thin PTFE sheets or fluoroplastics. Lining carbon steel tanks with thin PTFE or fluoroplastic sheets is the best way to make inexpensive, highly corrosion-proof tanks. |
|  | Advantages: The application of PTFE-lined technological facilities or units in the chemical, petrochemical, pharmaceutical and food industries ensures high quality and purity of products, extended sevice life and easy maintenance of facilities. The unique properties of fluoropolymers have made them an indispensable material for any kind of modern equipment, applied in today's broad list of industries. |

|  | Expanded PTFE sealant for flange joints AVKOSEAL-AL |
| --- | --- |
|  | AVKOSEAL-AL is a sealant, manufactured from 100% pure expanded PTFE. It is typically produced as a tape and is less widely used in the form of a cord, plates etc. The expanded PTFE comprises all the exceptional operation parameters of PTFE plus the additional features acquired in the process of expansion. To facilitate the fitting AVKOSEAL-AL is provided with a one-sided adhesive backing strip with protective layer made from special paper, which is removed before fitting. Due to its excellent flexibility and ductility AVKOSEAL follows very easily the shape of the sealed surface, and the adhesive strip enables the quickness of the fitting. Apart from the flange sealing AVKOSEAL-AL may be successfully used in every other case of static sealing, provided that the working parameters fall into the range PTFE's values. Sizes and lengths in one reel: Standard size Standard size Length in roll Standard size Standard size Length in roll mm Ø mm m mm Ø mm m 1 50 100 14 x 5.0 14 6 20 3 x 1.5 3 30 60 17 x 6.0 17 5 20 5 x 2.0 5 25 50 20 x 7.0 - 5 20 7 x 2.5 7 20 40 22 x 5.0 - 5 20 10 x 3.0 10 10 40 25 x 5.0 - 5 20 12 x 4.0 12 7.5 25 28 x 5.0 - 5 20 |
|  | Advantages of the material |
|  | Chemical resistance to almost all aggressive mediums (РН range 0 - 14); Temperature range: from - 240 °С to +290 оС, short periods up to 310 оC; Physiologically safe - without taste and smell, nontoxic, does not contain soluble components, not influenced by microorganisms (moulds); Ensures cleanness of the medium; Hydrophobic, non ageing, resistant to UV - unlimited operational validity; In working conditions AVKOSEAL-AL does not change its hardness and brittleness; Nonflammable and noncombustible; Short fitting time, since AVKOSEAL-AL is ready for application and is not made from sheet material; Quick disassembly: AVKOSEAL-AL may be easily removed, without traces; No need of cutting (moulding) of the sealing; Complete use: no waste material; No need of additional mechanical treatment of the surfaces sealed: AVKOSEAL-AL is easily adapted and compensates deviations from shape and condition of the surface; The flexibility of AVKOSEAL-AL allows sealing of the most complicated configurations; Small storage costs - the material is packed in reels, as only several of them are sufficient for any sealing applications. |

Thermo-insulating materials Heat isolation of machines, devices and energy transporting installations in the industry is of crucial importance for increasing of the energy effectiveness, achieving longer exploitation terms of the industrial equipment and preserving the operational personnel from health hazards. The thermo isolating materials of AVKO jsc are based upon silicate fibers and for more than a decade now work successfully as a substitute for the asbestos products when working under extreme high temperatures (1000 ÷ 1200 °C). The great diversity of thermo isolating products offered by AVKO jsc makes possible the solving the of any isolation problem. To guarantee the quality of its products AVKO jsc may present The Golden Medal received at the International Technical Fair in Plovdiv in1997 for a series of silicate products.

Textile thermo-insulating materials AVKOTHERM® 52, AVKOTHERM® 62 - Thermo-insulating clothes Thermo-insulating cloths produced on the basis of ceramic fibres are designed primarily for heat insulation, protection in case of fire related jobs (such as welding, gas cutting), production of thermal protection screens, devices and clothing. The cloths have the following advantages: regular structure, resistant to burning out, same strength in weft and warp. AVKOTHERM® 52 62 C 62 C/AR 62 T 62 T/AR Description Glass cloth Ceramic cloth medium type Ceramic cloth medium type, reinforced with metal wire Ceramic cloth heavy type Ceramic cloth heavy type reinforced with metal wire Standard width 1000 ± 20 mm 1000 ± 20 mm 1200 ± 20 mm 1000 ± 20 mm 1200 ± 20 mm 1000 ± 20 mm 1200 ± 20 mm 1000 ± 20 mm 1200 ± 20 mm Surface density 1000 ± 50 g/m2 1000 ± 50 g/m2 1100 ± 50 g/m2 1400 ± 50 g/m2 1460 ± 50 g/m2 Thermal resistance 450 °C 980 °C 1200 °C 980 °C 1200 °C AVKOTHERM® 54, AVKOTHERM® 64 - Thermo-insulating tapes The thermo-insulating tapes AVKOTHERM® 54 (series glass tapes) and AVKOTHERM® 64 (series ceramic tapes) find application as universal insulations in a wide range of industrial fields. Used basicaly for: insulation of cables and pipelines; insulation of gates of fireplaces, boilers and furnaces and in special manufacturing processes, for example outer coating of transport bands in glass industry and elsewhere. Thermo-insulating tapes are made in standard widths from 20 to 320 mm. AVKOTHERM® 63 - Fire-extinguishing blankkets The fire-extinguishing blankets AVKOTHERM® 63 are designed on the dasis of siliceous heat insulating cloths and serve for protection from fire in places, where it is not recommended to apply water, foam, etc. Those find application for covering parts of industrial systems or electrical cable, if located nearby fire hazard high temperatures; as well as for fire extinguishing in premises containing easy flammable and explosive substances - studios, laboratories; for protection of people against fire and others. Sizes 1200 x 1800 mm Mass 2.3 kg Humidity 1.3 % Flexibility without residual deformation Dielectric strength > 1 MW Number of fibers per 10 cm - on warp 72 ± 2 - on weft 28 ± 2 Fire extinguishing effect for sunflower oil extinguishes Resistance to moths and microorganisms resistant Thermo-insulating cords The thermo-insulating cords manufactured from siliceous fibers are mainly used for heat insulating of pipelines carrying steam, heaters, industrial equipment, etc. working at high temperature. It is suitable for static sealing of lids, hatches, doors, etc. and also sealing of furnaces, boilers, ventilators, etc. AVKOPACK® 501 Technical data in PDF format Composition Тwisted cord made from textured glass yarn Working temperature 450 °C Density 0.6 ± 10 % AVKOPACK® 501H Technical data in PDF format Composition Cord made of glass fibers, reinforced with outside hose made of glass and cotton yarn with surface processed with special system of silicate materials Working temperature 700 °C Density 0.6 ± 10 % AVKOPACK® 503 EKO Technical data in PDF format Composition Ecorope, braided from ceramic fibers with inner core from ecoproduct from ceramic with content of Al2O3 < 1% Working temperature 1100 °C Density Ø35 - 0.3 ±10 % ; Ø80 - 0.16 ±10 % AVKOPACK® 505 Technical data in PDF format Composition Elastic cord braided of textured glass yarn Working temperature 500 °C Density 0.6 ± 10 % AVKOPACK® 600/600AR Technical data in PDF format Composition Twisted cord made from ceramic yarn and basic fibres made of glass or steel. The cord is produced with filling of ceramic yarn or silicate material Working temperature 980 / 1200 °C Density 0.5 ± 10 % AVKOPACK® 601 Technical data in PDF format Composition Cord made of silicate filling and dense glass braiding Working temperature 1000 °C Density 0.5 ± 10 % AVKOPACK® 603 Technical data in PDF format Composition Cord made of parallel ceramic fibres firmly braided with inconel fibre Working temperature 1200 °C Density 0.55 ± 10 % AVKOPACK® 506, AVKOPACK® 606 - Glass and ceramic hollow sealing sleeves Advanced sealing product braided from: textured or filament glass yarn; ceramic yarn with glass or metal bearing wire; Working temperature glass sleeve 550 °C ceramic sleeve with glass fiber 980 °C ceramic sleeve with metal fiber 1200 °C Standard sizes glass sleeves Ø10, Ø12, Ø14, Ø15, Ø20, Ø25, Ø30, Ø35, Ø40 ceramic sleeves Ø20, Ø25, Ø30, Ø35, Ø40 Wall thickness glass sleeves 1 ÷ 3 ceramic sleeves 2 ÷ 4

# Thermal insulation mattresses for multiple use

## AVKOTHERM® 57 - Thermal insulation mattresses for multiple use

## Description

АВКОТЕРМ® 57 is a multi-layered insulation with thermal- resistant textile casing attached by arresting springs. Over the outer surface of the clothing are situated fastening together elements that prove the stability of fixing the clothing to the insulating object.

The elaboration differs with its specific method of approach to every different type of the insulation object, referring its adaptability to work at different exploitation conditions and working media temperatures from -25 to 1100°С, high content of humidity, acids or other aggressive fluids, as well as characteristics of the atmospheric conditions.

## Applications

Applications:

- Fixture

- Flanges

- Tanks

- Steam generators

- Heat exchangers

- Vessels under pressure

- Flexible joints

- Valves

- Pumps

- Turbines

- Ventilators

- Non-standard equipment

## Advantages

- Energy saving - considerable level of decreasing the heating losses;

- Possibility to be used in a wide temperature range from -25 to 1100 °С;

- The construction could be tight for liquids and not to attain them in its volume;

- Resistance to abrasives

- Allows a repeated mounting and dismantling, without changing the parameters characterizing the quality of the product;

- Quick and easy mounting and dismantling, without using instruments;

- Comparatively lower weight from the other insulating constructions;

- Vibration-resistance - reliable fixing and flexibility to АВКОТЕРМ® 57 provides invariability of the disposition;

- Noise insulation;

- Fire protection - the materials used in the constructions working above 200°C - 250 °C are incombustible. Following a request a construction with combustible materials could be elaborated and at lowered temperatures, too;

- Protection of the staff servicing from incineration. The temperature of the surface is not exceeding 45 °C, at 25 °C of the environment;

- After a request specific conditions of exploitation are reported, which guarantees free of all average work and long life of the product.

Thermo-insulating boards AVKOTHERM® 65 and AVKOTHERM® 65/1 The thermo-insulating boards AVKOTHERM® 65 and AVKOTHERM® 65/1 are complete non-asbestos material. They are made of inorganic mineral fibres with a limited quantity of fillings. They are especially appropriate for sealing manufacture of various sizes, used for heat insulation under high temperatures. AVKOTHERM® 65 AVKOTHERM® 65/1 Standard sizes 1000 x 1000 mm 1000 x 1000 mm Standard thickness 1.5 - 10 mm 1.5 - 10 mm Working temperature 850 °C 1200 °C Tensile strength (DIN 52910) 3.00 N/mm2 3.30 N/mm2 Specific weight (DIN 3752) 1.00 g/cm3 0.90 g/cm3 Thermal conductivity (at 400°C) 0.100 W/mK 0.100 W/mK

# Thermoinsulation materials made of basaltic mineral wool

## AVKOTHERM® 65 and AVKOTHERM® 65/1

## General properties

- Inorganic product, obtained from basaltic mineral fibers;

- Non combustible and not inflammable;

- Fonoisolating;

- Chemical inert, does not attack other materials, is not corroded by other materials;

- Is not toxic, does not pollute the environment;

- Does not age, does not rot;

- Thermo isolating up to 700 °C;

- Does not change its shape and dimensions;

- Easy to handle and work with it;

- The product is waterproof;

## Field of application

- Thermal and fono-isolation, protection against fire, when used in construction with horizontal or vertical surfaces;

- Thermal isolation of district heating pipes in civilian and industrial installations;

- The production of isolating panel, suspended roof, partition panel;

- Thermal isolation of channel from refrigerating chambers;

- Thermal isolation for industrial installation, ships, train wagon, frigorific cars and chambers;

- Thermal and fono isolation of prefab houses, partition walls, curtain walls, facade;

- Thermal and fono isolation of passable terrace, (with suitable precautions), and roofs.

## Technical Specification

Download the technical data in PDF

AVKO JSC preserves the right to make any changes to the product and respectively its technical characteristics at any time.

Tehermo-insulating cladding AVKOTHERM® 66/11 AVKOTHERM® 66/11 is specially developed mixture of inorganic mineral fibers, cement and chemically inert fillers. After stirring with water, this composition forms a defensive cladding with common usage and self-drying effect. It is used for spreading on a ready thermoinsulation with a steel wire web fixed on it. The cladding prevents the already put thermoinsulation from atmospheric and mechanic influence. Pain, ferolites and other organic claddings may be spread on it. Dansity 1300 kg/m3 Working temperature 120 - 700 °C Compression strength 20 - 25 MPa Tensile strength 6 - 7 MPa Thermal conductivity coefficient (at 25 °C) 0.28

|  | ELECTROINSULATING MATERIALS |
| --- | --- |
|  | AVKOLIT 551 (PHENOLIC GLASS CLOTH LAMINATED SHEETS) |
|  | The phenolic glass cloth laminated sheets are laminated material, made through the hot pressing of two or more layers of alkali-free glass material (with unbroken fibre), reinforced with thermoreactive resin of phenol or epoxide type. * Delivery at request of copper-folio-faced phenolic glass cloth laminated sheets. |
|  | AVKOLIT 451 (PHENOLIC COTTON CLOTH LAMINATED SHEETS) |
|  | The phenolic cotton cloth laminated sheets are made by a laminated material through the hot pressing of two or more layers of cotton fabric, reinforced with synthetic thermoreactive resins of phenol-formaldehyde type, cresol-formaldehydes, mixture of these resins or their modifications. |
|  | AVKOLIT 452 (PHENOLIC COTTON CLOTH LAMINATED ROD) |
|  | The phenolic cotton cloth laminated rods with circular section are made through pressing of cotton fibre in a pressform, reinforced with thermoreactive resin of phenol type. |
|  | AVKOLIT 851 (PHENOLIC PAPER LAMINATED SHEETS) |
|  | The phenolic paper laminated sheets is a layered material, made through the hotpressing of two or more layers of electroinsulating paper, reinforced with synthetic thermoreactive resins of phenol-formaldehyde and cresol-formaldehyde type, mixture of these resins or their modifications. |
|  | The surface area of all materials is plain, smooth, evenly painted in natural color, without air or gas bubbles and current-carring switches. They can be mechanically treated: cut, drilled, turned on a lathe, milled, punched with no occurrence of cracks or dislodges. |
|  | TECHNICAL PARAMETERS |
|  | AVKOLIT 551 AVKOLIT 451 AVKOLIT 452 AVKOLIT 851 Size 1980 x 980 ?10 mm 1980 x 980 ?10 mm 1000 ? 5 mm 1980 x 980 ?10 mm Thicknesses (diameters) 0.4 ÷ 50 mm 0.8 ÷ 50 mm Ø6 ÷ Ø200 0.4 ÷ 50 mm Density 1.7 ÷ 1.9 g/cm3 1.3 ÷ 1.4 g/cm3 1.32 ÷ 1.39 g/cm3 1.3 ÷ 1.4 g/cm3 Flexural strength perpendicular to lamination > 340 MPa > 70 MPa > 88 MPa > 90 MPa Bonding strength > 5500 N > 2800 N Notch impact strength parallel to lamination (Charpy) > 33 kJ/m2 Dielectric strength perpendicular to lamination (in oil 90 ? 2 ? C ) > 14,2 MV/m > 2 MV/m (1.5-2 mm) > 12 MV/m Breakdown voltage parallel to lamination (in oil 90 ? 2 ? C ) > 35 kV Breakdown voltage parallel to lamination (in transformer oil 20 ? 5 ? C ) > 10 kV > 10 kV Insulation resistance after impregnated in water > 5x108Om Insulation resistance parallel to the lamination > 1x108Om > 1x109Om |

|  | COMPRESSED JOINTING SHEETS |
| --- | --- |
|  | :: NA 202 (red colour) |
|  | Oil-resistant rubber composed by organic fibres, NBR, for light to medium load pressure. Very suitable for use in the automotive and food industry. |
|  | :: NA Extra (dark green colour) |
|  | Jointing sheet composed by synthetic fibres with rubber, suitable for use in air, water and unagressive areas. |
|  | :: AVKOPRESS G (green colour) |
|  | Jointing sheet composed by high quality synthetic fibres and rubber systems. Suitable for use in air, water and unagressive areas. It is applicable in flange sealing, front surfaces etc. |
|  | :: AVKOPRESS B (blue colour) |
|  | Jointing sheet composed by high quality synthetic fibres and rubber systems. Suitable for use in air, water and unagressive areas. It is applicable in flange sealing, front surfaces etc.. |
|  | Technical parameters Type NA 202 NA Extra AVKOPRESS G AVKOPRESS B Size, mm 1500x1500 1500x1500 1500x2000 1500x2000 Thickness, mm 0.5; 0.8; 1.0; 2.0; 3.0 0.5; 0.8; 1.0; 2.0; 3.0 0.5; 1.0; 1.5; 2.0; 2.5; 3.0; 4.0; 5.0 0.5; 1.0; 1.5; 2.0; 2.5; 3.0; 4.0; 5.0 Max. temperature*,°C 180 290 300 360 Max. temperature with steam*,°C 120 260 250 300 Max. pressure*, bar 40 100 45 60 Specific weight ,g/cm3 1.8 +1% 1.75 +1% 1.9 +1% 1.9 +1% Shrinkage,% 8 7 11 12 Recovery,% 50 55 52 58 Tensile strength, MPa 7 7 8 10 |
|  | * The values of the temperature and the pressure are maximal. The using of the material at maximal values of the indices together is not recommended. These values are approximate and depend not only on the type of the sealing material but on additional factors, like the conditions of mounting. Very important parameters are the thickness of the sheet, the type of the fluid, the type of the flange and the surface tensions. Their use in vapor requires special technical attention. |
|  | Compressed Jointing Sheets are attended by "Gasket installation procedures" recommended from ESA (European Sealing Association). Download: Gasket installation procedures |
|  | :: FINISHED FLAT GASKETS |
|  | The finished flat gaskets are produced from non-asbestos jointing sheets, described in this brochure. The goods are available in wide range of dimensions covered, according to DIN 2690, DIN 2691, DIN 2692, specially for shipbuilding industry 3Н-632-92 and non-standart sizes on request. Features: - lack of processing wastes; - economy of money and time; - high quality. |
|  | :: DEVICE FOR CUTTING OF FINISHED GASKETS |
|  | The device intended for cutting of gaskets from sheet packed material. It allows a maximum usage of the material and meanwhile is very suitable and easy running. Maximum diameter when making a gasket with fixing of the semifinal product in the center of the work board - ø500 мм. Maximum diameter, when making a gasket with fixing of the semifinal product in the corner of the work board - ø1000 мм. |

|  | TECHNICAL RUBBER SHEET |
| --- | --- |
|  | Technical parameters |
|  | rubber ordinery sheet rubber oil resistance sheet rubber acid resistance sheet rubber thermal resistance sheet Width mm 1000 1000 1000 1000 Thicknesses mm 1 ÷ 20 1 ÷ 20 1 ÷ 20 1 ÷ 20 Density g/cm3 1.5 ÷ 2% 1.5 ÷ 2% 1.5 ÷ 2% 1.5 ÷ 2% Tensile strength MPa 4.1 5.6 4.8 6.1 Broken extension rate % 280 260 260 300 Hardness 75 72 68 73 Weight increasing after dipping in petrol+benzene (75:25) % 16.5 Weight increasing after dipping into industrial oil for transformer % 6.8 Ageing rate 20% H2SO4, 23 °C + 24 h 20% NaOH, 23 °C + 24 h % 0.8 0.8 Recommended work temperature °C 80 - 100 Instant temperature °C 200 |

|  | FRICTION MATERIALS |
| --- | --- |
|  | Non-asbestos brake textile |  |
|  | Composition A synthetic textile, made of kevlar and glass fibers, reinforced with copper fiber and steeped in impregnation mixture. Application In braking gears of ropeways, traction engines, excavators, cranes and other hoists. Technical characteristics Working temperature -300°C Water absorption for 24 hours max. 18% Friction coefficient min 0,20 Linear wear max. 0.22 mm/2h Dimensions width from 40 till 260 mm thickness from 4 till 25 mm Roll length from 10 till 15 m |
|  | Automobile plates Cone rings for motor-cultivators |

|  | PREVECTRON® 2 - E. S. E. Lightning Conductors |
| --- | --- |
|  | AVKO JSC offers lighting-protectors PREVECTRON® 2, produced by INDELEC® - France and we are the one and only representative for Bulgaria of this product. |
|  |  |  | Key benefits The skills of INDELEC’s engineers, the variety of tests carried out in both high-voltage laboratories and real-life lightning conditions, and the experience gained from the thousands of PREVECTRON®2 installations around the world, have allowed us to develop a complete range of lightning conductors offering a host of key benefits: |
|  |  |  | 6-model range offering customized solutions for each project (easthetic constraints, required protection area, etc.) fully autonomous operation total reliability, even in extreme climatic conditions proven, robust design able to withstand multiple lightning strikes lightning conductor only becomes active when electrical field intensity rises (lightning discharge likely), the PREVECTRON®2 presents no danger to the site straightforward installation & maintenance using tools specially developed by INDELEC, including protection calculation software, strike counter and PREVECTRON® tester high-voltage laboratory test results available on request real-life test results & scientific reports available on request ultra-safe capture tip thanks to full electrical continuity between the tip and the earth point ISO 9001-2000 manufacturing process (certificate No.116884) |
|  |  |  | Protection area The protection area Rp of a PREVECTRON®2 lightning conductor is calculated according to French Standard NF C 17-102, thus The protection area depends on a number of factors: |
|  |  |  | Gain in triggering time T(µs) of the chosen PREVECTRON®2 L(m) = V(m/µs); V* = 1 m/µs T* S 6.60 S 4.50 S 3.40 TS 3.40 TS 2.25 60 50 40 40 25 * values obtained through tests conducted in high voltage laboratories. D(m) = 20, 45, or 60, depending on the protection level required (I, II, or III) on a given site, according to the lightning risk assessment guide. the actual height of the lightning air terminal above the surface to be protected: h (where h < 5 m, for Rp see table below). |
|  |  |  | Protection Radii |
|  |  |  | Level I : D=20m high protection h(m) 2 3 4 5 10 S 6.60 31 47 63 79 79 S 4.50 27 41 55 68 69 S 3.40 23 35 46 58 59 TS 3.40 23 35 46 58 59 TS 2.25 17 25 34 42 44 TS 2.10 10 15 21 26 26 |
|  |  |  | Level II : D=45m medium protection h(m) 2 3 4 5 10 S 6.60 39 58 78 97 99 S 4.50 34 52 69 86 88 S 3.40 30 45 60 75 77 TS 3.40 30 45 60 75 77 TS 2.25 23 34 46 57 61 TS 2.10 15 22 30 38 38 |
|  |  |  | Level III : D=60m standard protection h(m) 2 3 4 5 10 S 6.60 43 64 85 107 109 S 4.50 38 57 76 95 98 S 3.40 33 50 67 84 87 TS 3.40 33 50 67 84 87 TS 2.25 26 39 52 65 69 TS 2.10 17 26 34 43 44 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Woodworking copying lathes R-110 и R-154 |
|  | Technical specifications R - 110 R - 154 Distance between centres mm 1100 1500 Centres height mm 230 230 Front spindle end -outer thread M33 DIN 800 M60 DIN 800 -cylindrical hole ø20 H7/M12 ø36 H7/34 Spindle rotation speed min-1 720, 1150, 1750, 2800 650, 1000, 1800, 3000 Tailstock MK2 MK2 Copying length mm 1000 1350 Copying diameter mm ø100 ø100 Motor power kW 0.75 1.5 Overall dimensions length mm 1700 2350 width mm 500 550 height mm 1140 1165 weight kg 120 400 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Universal band saw machines BU 634, BU 804 |
|  |  | Technical specifications BU 634 BU 804 Drive wheel diameter mm 630 800 Max. cutting height mm 380 450 Distance between the saw blade and the body mm 610 780 Max. saw blade length mm 4700 5750 Max. saw blade width mm 32 40 Max. saw blade thickness mm 0.6 0.8 Blade speed m/s 28 28 Table dimensions mm 630 - 710 850 - 900 Table tilting ° 0 - 45 0 - 45 Motor power kW 4 4 Overall dimensions length mm 1200 1150 width mm 1000 1100 height mm 2160 2500 weight kg 650 750 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Band saw welding machine AZL 403 |
|  | Technical specifications Range of welded bandsaws for wood cutting width mm 10 ÷ 50 thickness mm 0.4 ÷ 0.9 Range of welded bandsaws for metal cutting width mm 10 ÷ 25 thickness mm 0.5 ÷ 0.9 Range of welded bimetallic bandsaws width mm 10 ÷ 25 thickness mm 0.5 ÷ 0.9 Power consumption kW 4.5 Protection rating IP 22 Overall dimensions length mm 500 width mm 340 height mm 430 weight kg 52 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Grinding machine for circular end band saw MZ 101 |
|  | Technical specifications Abrasive disk diameter mm ø 200 Disk speed min-1 3000 Abrasive disk tilting ° -5 to +15 Grinded teeth per minute 72 Diameter of the grinded saw blade mm ø 100 ÷ ø 400 Band saw width mm 16 ÷ 80 Tooth pitch mm 5 ÷ 25 Tooth depth mm 2.5 ÷ 12.5 Motor power kW 0.55 Overall dimensions length mm 600 width mm 300 height mm 300 weight kg 59 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Saw Sawage ACHL 401 |
|  |  | Technical specifications Band saw width mm 6 ÷ 50 Band saw thickness mm 0.4 ÷ 0.9 Tooth pitch mm 3 ÷ 20 Clasping schemes 1) left-right-left-right 2) left-right-straight Overall dimensions length mm 250 width mm 210 height mm 250 weight kg 16 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Belt sanding machine MSL 244 |
|  | Technical specifications Table length mm 2400 Table width mm 800 Max. belt length mm 7100 Min. belt width mm 6900 Belt width mm 120 Pulley diameter mm 300 Belt speed m/s 22 Motor power kW 4 Overall dimensions length mm 3600 width mm 1300 height mm 1345 weight kg 320 |
|  | :: Belt sanding machine MSL 083 |
|  | Technical specifications MSL 083 Table length mm 800 Table width mm 225 Belt length mm 2250 Belt width mm 120 Pulley diameter mm 128 Belt speed m/s 11 Table tilting ° 0 - 45 Belt oscillation mm 36 Motor power kw 1.5 Overall dimensions length mm 1200 width mm 450 height mm 1100 weight kg 100 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Circular saw blade machine CDR 700 |
|  | Technical specifications Saw blade diameter mm ø 700 Wood cutting diameter mm max. 200 Motor speed min-1 1450 Motor power kW 4 Overall dimensions length mm 1000 width mm 1000 height mm 1000 weight kg 95 |

|  | WOODWORKING MACHINES |
| --- | --- |
|  | :: Circular saw blade cutter CMN 301 |
|  | Technical specifications Circular saw blade diameter mm ø 300 Clamp capacity mm 160 Circular saw blade inclination ° - 45 to +45 Circular saw blade speed min-1 50 / 100 Cutting possibilities: at 45 ° 90 50 80 x 80 70 x 110 Motor power kW 1.5/2.2 Overall dimensions length mm 1500 width mm 1150 height mm 1000 weight kg 180 |